PRESSED POWDER 
Description: A pressed powder that feels silky smooth but also very “cohesive” and non powdery.  It imparts a very natural finish to the skin.  To be applied with a dry sponge.

Part  
CTFA Name 



Trade Name 

% 
Supplier

A. 
Sericite 



SERICITE J 

35.00 
KOBO 

Talc (and) Lecithin 


TALC A-CL3 

35.00 
KOBO

Yellow Iron Oxide (and) Isopropyl
BYO-I2 

  0.88 
KOBO 

Titanium Triisostearate 

Red Iron Oxide (and) Isopropyl
BRO-I2 

  0.76 
KOBO 


Titanium Triisostearate 


Black Iron Oxide (and) Isopropyl
BBO-I2 

  0.36 
KOBO

Titanium Triisostearate 

B.
Pentaerythritol Tetraoctanoate 
PE48 


  8.00 
KOBO
C. 
Hexyldecyldiisocyanate/ 

DPD-500 

20.00
KOBO

Trimethylol Hexlace Crosspolymer 



-------- 


and silica. 






100.00
Procedure: Pass the pre-mixed Part A through pulverizer until color is fully developed.  Spray the pre-warmed (65-70˚C) Part B and mix well.  Pass through a pulverizer until oil is completely dispersed.  Add Part C and blend well.  If necessary, pass through a pulverizer.  Do not overheat.
