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Phase 1

Castor Oil 47.92

Citric Acid (USP Grade) 0.1

C14-026 SunCroma D&C Red 27 0.03 SunChemical

C14-032 SunCroma D&C Red 21 3 SunChemical

C33-500 SunCroma Black Iron 0.6 SunChemical

Phase 2

Candelilla Wax 7

Ozokerite Wax 3

Beeswax 4

Carnauba Wax 4

Acetylated Lanolin Alcohol and Cetyl Acetate 8

Lanolin Oil 10

Hydrogenated CocoGlycerides 7

Octyldodecanol 5

Phase 3

Metylparaben 0.2

Propylparaben 0.1

BHT 0.05

Total 100
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CA 1031 Gray Mood Lipstick
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Process: 

1. Premix pigments and citric acid into sufficient castor oil (Phase 1) and disperse through 3-roll mill twice.

2. Mix and melt all wax and oil ingredients (Phase 2), heating to 80-85oC.

3. Mix in preservatives (Phase 3) until fully dispersed.

4. Add pre-milled pigment / citric acid / castor oil from Step 1. Mix until homogenous.

5. Cool batch to 55-60oC and pour into molds.
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 
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		Ingredients		%(w/w)		Functions		INCI designation		Supplier

		Phase 1

		Castor Oil		47.92

		Citric Acid (USP Grade)		0.1

		C14-026 SunCroma D&C Red 27		0.03						SunChemical

		C14-032 SunCroma D&C Red 21		3						SunChemical

		C33-500 SunCroma Black Iron		0.6						SunChemical

		Phase 2

		Candelilla Wax		7

		Ozokerite Wax		3

		Beeswax		4

		Carnauba Wax		4

		Acetylated Lanolin Alcohol and Cetyl Acetate		8

		Lanolin Oil		10

		Hydrogenated CocoGlycerides		7

		Octyldodecanol		5

		Phase 3

		Metylparaben		0.2

		Propylparaben		0.1

		BHT		0.05

		Total		100






