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Phase 1

Deionised water 56.15

Propylene Glycol 6.5 Emollient

Ultrez 20 0.3 Gelling agent

NaOH(20% Solution) 0.15 Neutralizer

Phase 2

Apifil 2 o/w emulsifier PEG-8 Beeswax Gattefosse

Compritol 888 ATO 4 Compacting agent Glyceryl 

Dibehenate/Tribehenin/Glyceryl 

Behenate

Gattefosse

Microcrystalline Wax 1 Thickener

Corum 2340 4 Emollient Glyceryl Stearate Corum

Florasun 90 2 Emollient Helianthus Annuus (Sunflower) 

Seed Oil

Floratech

Cetyl Alcohol 3.6 Thickener

Stearic Acid 1 Thickener

Silsurf J208 3.8 Feeling agent PEG-8 Dimethicone Siltech

Syntran PC 5112 15 Quick Setting Agent Interpolymer

Phase 3

Microcare MTP 0.2 Preservatives

Fragrance 0.3 Perfume Technico Flor

Total 100


[image: image3.png]






CA 1043 Hair Wax
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Process: 

1. Add Propylene Glycol into water and stir until homogenous. Then disperse Ultrez 20 over the water. Let stand.

2. Then, add NaOH to adjust the pH of the system within 6.5-7.

3. Add Phase 2 heated to 80oC to Phase 1 heated to 80oC.

4. Finally, add Phase 4 into the mixture when the temperature of the mixture cooled down below 40oC and stir until homogenous.
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 
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		Ingredients		%(w/w)		Functions		INCI designation		Supplier

		Phase 1

		Deionised water		56.15

		Propylene Glycol		6.5		Emollient

		Ultrez 20		0.3		Gelling agent

		NaOH(20% Solution)		0.15		Neutralizer

		Phase 2

		Apifil		2		o/w emulsifier		PEG-8 Beeswax		Gattefosse

		Compritol 888 ATO		4		Compacting agent		Glyceryl Dibehenate/Tribehenin/Glyceryl Behenate		Gattefosse

		Microcrystalline Wax		1		Thickener

		Corum 2340		4		Emollient		Glyceryl Stearate		Corum

		Florasun 90		2		Emollient		Helianthus Annuus (Sunflower) Seed Oil		Floratech

		Cetyl Alcohol		3.6		Thickener

		Stearic Acid		1		Thickener

		Silsurf J208		3.8		Feeling agent		PEG-8 Dimethicone		Siltech

		Syntran PC 5112		15		Quick Setting Agent				Interpolymer

		Phase 3

		Microcare MTP		0.2		Preservatives

		Fragrance		0.3		Perfume				Technico Flor

		Total		100






