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Phase 1

Deionised water 43.41

Lucentite SWN 2 Suspending agent Lithium Magnesium Sodium 

Silicate

Kobo

Phase 2

Deionised water 20

Disodium EDTA 0.1 Chelating agent

Xanthan Gum 0.4 Gelling agent

Phase 3

WE 70U 6 Coloring agent Titanium Dioxide (and) 

Polyglyceryl-4 Isostearate (And) 

Cetyl PEG/Ppg-10/1 

Dimethicone (And) Hexyl Laurate 

(and) Isopropyl Titanium 

Triisostearate

Kobo

WE 55Y 0.23 Coloring agent Iron Oxide (CI 77492) (and) 

Polyglyceryl-4 Isostearate (And) 

Cetyl PEG/Ppg-10/1 

Dimethicone (And) Hexyl Laurate 

(and) Isopropyl Titanium 

Triisostearate

Kobo

WE 70R 0.05 Coloring agent Iron Oxide (C.I. 77491) (And) 

Polyglyceryl-4 Isostearate (And) 

Cetyl PEG/Ppg-10/1 

Dimethicone (And) Hexyl Laurate 

(and) Isopropyl Titanium 

Triisostearate

Kobo

WE 70B 0.01 Coloring agent Iron Oxide (C.I. 77499) (And) 

Polyglyceryl-4 Isostearate (And) 

Cetyl PEG/Ppg-10/1 

Dimethicone (And) Hexyl Laurate 

(and) Isopropyl Titanium 

Triisostearate

Kobo

Cocoate BG 4 Wetting agent Butylene Glycol Cocoate Gattefosse
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CA 1053 Water Proof Liquid Foundation
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Phase 4

SPCAT-I2 1 Feeling agent Talc (and) Ethylene Mathacrylate 

Copolymer (and) Isopropyl 

Titanium Triisostearate

Kobo

ASO-I2 1 Mattifying agent Aluminium Starch 

Octenylsuccinate (and) Isopropyl 

Titanium Triisostearate

Kobo

SP-500 1 Feeling agent Nylon-12 Kobo

Sunshine Glitter White 

C80-3400

1 Effect pigment Fluorphogopite (and) Titanium 

Dioxide

Sun 

Chemical

Phase 5

Hydrolactol 70 4 O/W emulsifier Glyceryl Stearate (and) 

Propylene Glycol Stearate (and) 

Glyceryl Isostearate (and) 

Propylene Glycol Isostearate 

(and) Oleth-25 (and) Ceteth-25

Gattefosse

Isostearyl Isostearate 4 Emollient Isostearyl Isostearate Gattefosse

BC Volatile 5 6 Feeling agent Cyclomethicone Basildon

BC 100cS 1 Feeling agent Dimethicone Basildon

Phase 6

Microcare MTP 0.2 Preservatives

PF. CORS 10602  0.6 Fragrance Technico 

Florasun 90 2 Emollient Sunflower Oil Floratech

Siltech CE-2000 2 Feeling agent Trioctyldodecyl citrate Siltech

Total 100


Process: 

1. Disperse Lucentite SWN over the water. Let stand.

2. Dissolve Disodium EDTA and disperse Xanthan Gum over the water. Let stand.

3. Add Phase 1 into Phase 2 and stir until homogeneous.

4. Wet WE 70U, WE55Y, WE 70R and WE70B with Cocoate BG and stir until homogeneous.

5. Add Phase 4 into Phase 3 and stir until homogenous.

6. Then, add Phase 5 into Phase 3+4.

7. Add Phase 3+4+5 heated to 75-80oC into Phase 1+2 heated to 75-80oC with moderate stirring.

8. Cool while stirring.

9. Add in Phase 6 into Phase 1+2+3+4+5 at about 45-50oC and stir until homogenous.[image: image3.jpg]



This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 
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		Ingredients		%(w/w)		Functions		INCI designation		Supplier

		Phase 1

		Deionised water		43.41

		Lucentite SWN		2		Suspending agent		Lithium Magnesium Sodium Silicate		Kobo

		Phase 2

		Deionised water		20

		Disodium EDTA		0.1		Chelating agent

		Xanthan Gum		0.4		Gelling agent

		Phase 3

		WE 70U		6		Coloring agent		Titanium Dioxide (and) Polyglyceryl-4 Isostearate (And) Cetyl PEG/Ppg-10/1 Dimethicone (And) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE 55Y		0.23		Coloring agent		Iron Oxide (CI 77492) (and) Polyglyceryl-4 Isostearate (And) Cetyl PEG/Ppg-10/1 Dimethicone (And) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE 70R		0.05		Coloring agent		Iron Oxide (C.I. 77491) (And) Polyglyceryl-4 Isostearate (And) Cetyl PEG/Ppg-10/1 Dimethicone (And) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE 70B		0.01		Coloring agent		Iron Oxide (C.I. 77499) (And) Polyglyceryl-4 Isostearate (And) Cetyl PEG/Ppg-10/1 Dimethicone (And) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		Cocoate BG		4		Wetting agent		Butylene Glycol Cocoate		Gattefosse

		Phase 4

		SPCAT-I2		1		Feeling agent		Talc (and) Ethylene Mathacrylate Copolymer (and) Isopropyl Titanium Triisostearate		Kobo

		ASO-I2		1		Mattifying agent		Aluminium Starch Octenylsuccinate (and) Isopropyl Titanium Triisostearate		Kobo

		SP-500		1		Feeling agent		Nylon-12		Kobo

		Sunshine Glitter White C80-3400		1		Effect pigment		Fluorphogopite (and) Titanium Dioxide		Sun Chemical

		Phase 5

		Hydrolactol 70		4		O/W emulsifier		Glyceryl Stearate (and) Propylene Glycol Stearate (and) Glyceryl Isostearate (and) Propylene Glycol Isostearate (and) Oleth-25 (and) Ceteth-25		Gattefosse

		Isostearyl Isostearate		4		Emollient		Isostearyl Isostearate		Gattefosse

		BC Volatile 5		6		Feeling agent		Cyclomethicone		Basildon

		BC 100cS		1		Feeling agent		Dimethicone		Basildon

		Phase 6

		Microcare MTP		0.2		Preservatives

		PF. CORS 10602 Creation Originale		0.6		Fragrance				Technico Flor

		Florasun 90		2		Emollient		Sunflower Oil		Floratech

		Siltech CE-2000		2		Feeling agent		Trioctyldodecyl citrate		Siltech

		Total		100
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		Ingredients		%(w/w)		Functions		INCI designation		Supplier

		Phase 4

		SPCAT-I2		1		Feeling agent		Talc (and) Ethylene Mathacrylate Copolymer (and) Isopropyl Titanium Triisostearate		Kobo

		ASO-I2		1		Mattifying agent		Aluminium Starch Octenylsuccinate (and) Isopropyl Titanium Triisostearate		Kobo

		SP-500		1		Feeling agent		Nylon-12		Kobo

		Sunshine Glitter White C80-3400		1		Effect pigment		Fluorphogopite (and) Titanium Dioxide		Sun Chemical

		Phase 5

		Hydrolactol 70		4		O/W emulsifier		Glyceryl Stearate (and) Propylene Glycol Stearate (and) Glyceryl Isostearate (and) Propylene Glycol Isostearate (and) Oleth-25 (and) Ceteth-25		Gattefosse

		Isostearyl Isostearate		4		Emollient		Isostearyl Isostearate		Gattefosse

		BC Volatile 5		6		Feeling agent		Cyclomethicone		Basildon

		BC 100cS		1		Feeling agent		Dimethicone		Basildon

		Phase 6

		Microcare MTP		0.2		Preservatives

		PF. CORS 10602 Creation Originale		0.6		Fragrance				Technico Flor

		Florasun 90		2		Emollient		Sunflower Oil		Floratech

		Siltech CE-2000		2		Feeling agent		Trioctyldodecyl citrate		Siltech

		Total		100






