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Phase 1

BTD-401 6.8 Titanium Dioxide (And) Isopropyl Titanium 

Triisostearate

Kobo

BYO-I2 0.4 Iron Oxide (C.I. 77492) (And) Isopropyl Titanium 

Triisostearate

Kobo

BRO-I2 0.2 Iron Oxide (C.I. 77491) (And) Isopropyl Titanium 

Triisostearate)

Kobo

BBO-I2 0.1 Iron Oxide (C.I.77499) (And) Isopropyl Titanium 

Triisostearate

Kobo

Cocoate BG 10 Butylene Glycol Cocoate Gattefosse

Phase 2

SunPearl Fine White 2

SPCAT-I2 3 Talc (and) Ethylene/Methacrylate copolymer (and) 

Isopropyl Titanium Triisostearate

Kobo

ASO-I2 13 Aluminium Starch Octenylsuccinate (and) Isopropyl 

Titanium Triisostearate

Kobo

Carnauba Wax 4

Microcrystalline Wax 1.5

Plurol Diisostearique CG 3 Polyglyceryl-3 Diisostearate Gattefosse

Labrafac CC 20 Caprylic/Capric Triglyceride Gattefosse

Preservatives 0.3

Phase 3

Water 34.9

Sodium Chloride 0.8

Total 100
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CA1066 Cream to Powder Foundation
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Process: 

1. Add Phase 1 raw material and mix with a homogenizer.

2. Add Phase 2 into Phase 1 and heat the mixture to 75-80oC with continuous agitation.

3. Add Phase 3 heated to 75-80oC slowly into the mixture and stir until homogenous.

4. Continue homogenizing to 55-60oC and fill into appropriate containers.
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 

Page 1 of 1
This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 

                                                                                                                                                                        Page 2 of 1                                                                                                                                                                        


_1303133622.xls
Sheet1

		Ingredients		% (w/w)		INCI Designation		Supplier

		Phase 1

		BTD-401		6.8		Titanium Dioxide (And) Isopropyl Titanium Triisostearate		Kobo

		BYO-I2		0.4		Iron Oxide (C.I. 77492) (And) Isopropyl Titanium Triisostearate		Kobo

		BRO-I2		0.2		Iron Oxide (C.I. 77491) (And) Isopropyl Titanium Triisostearate)		Kobo

		BBO-I2		0.1		Iron Oxide (C.I.77499) (And) Isopropyl Titanium Triisostearate		Kobo

		Cocoate BG		10		Butylene Glycol Cocoate		Gattefosse

		Phase 2

		SunPearl Fine White		2

		SPCAT-I2		3		Talc (and) Ethylene/Methacrylate copolymer (and) Isopropyl Titanium Triisostearate		Kobo

		ASO-I2		13		Aluminium Starch Octenylsuccinate (and) Isopropyl Titanium Triisostearate		Kobo

		Carnauba Wax		4

		Microcrystalline Wax		1.5

		Plurol Diisostearique CG		3		Polyglyceryl-3 Diisostearate		Gattefosse

		Labrafac CC		20		Caprylic/Capric Triglyceride		Gattefosse

		Preservatives		0.3

		Phase 3

		Water		34.9

		Sodium Chloride		0.8

		Total		100






