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Phase 1

ASO-I2 5.0 Powdery thickening 

agent

Aluminium Starch Octenylsuccinate 

(and) Isopropyl Titanium 

Triisostearate

Kobo

Sericite J 3.0 Filler Mica Kobo

MSS-500/3H 5.0 Silicone slip agent and 

absorbent

Silica Kobo

SP-500 4.0 Provides creamy feel 

and absorbent

Nylon-12 Kobo

SPCAT-I2 4.0 Improves skin feel and 

provides powdery after 

feel

Talc (and) Ethylene/Methacrylate 

copolymer (and) Isopropyl Titanium 

Triisostearate

Kobo

Phase 2

WE70U 10.0 Pigmentary grade 

dispersion (White)

Titanium Dioxide (and) Polyglyceryl-

4 Isostearate (and) Cetyl 

Dimethicone Copolyol (and) Hexyl 

Laurate (and) Isopropyl Titanium 

Triisostearate

Kobo

WE55Y 1.4 Pigmentary grade 

dispersion (Yellow)

Iron Oxide (CI 77492) (and) 

Polyglyceryl-4 Isostearate (and) 

Cetyl Dimethicone Copolyol (and) 

Hexyl Laurate (and) Isopropyl 

Titanium Triisostearate

Kobo

WE70R 0.5 Pigmentary grade 

dispersion (Red)

Iron Oxide (CI 77491) (and) 

Polyglyceryl-4 Isostearate (and) 

Cetyl Dimethicone Copolyol (and) 

Hexyl Laurate (and) Isopropyl 

Titanium Triisostearate

Kobo

WE70B 0.1 Pigmentary grade 

dispersion (Black)

Iron Oxide (CI 77499) (and) 

Polyglyceryl-4 Isostearate (and) 

Cetyl Dimethicone Copolyol (and) 

Hexyl Laurate (and) Isopropyl 

Titanium Triisostearate

Kobo
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CA1067 Cream to Powder Foundation with SPF15 
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TNP50VTTS 20.0 UV Filter C12-15 Alkyl Benzoate (and) 

Titanium Dioxide (and) Alumina 

(and) Polyhydroxystearate (and) 

Isopropyl Titanium Triisostearate 

(and) Triehoxy Caprylsilane

Kobo

BC20cs 6.0 Slip agent Dimethicone Basildon

Cocoate BG 10.0 Emollient Butylene Glycol Cocoate Gattefosse

Plurol Diisostearique 6.0 w/o, PEG-free  Polyglyceryl-3 Diisostearate Gattefosse

Compritol 888 ATO 0.5 Thickener for oils Glyceryl Dibehenate (and) 

Tribehenin (and) Glyceryl Behenate

Gattefosse

Carnauba Wax 4.0 Thickener  Copernicia Cerifera (Carnauba) 

Wax

Lipocire A 3.0 Emollients and 

improves skin feel

Hydrogenated Palm Kernel 

Glycerides (and) Hydrogenated 

Palm Glycerides

Gattefosse

Preservatives 0.3 Preservatives

Phase 3

Water 15.4

Salt 1.8 Stabilizer Sodium Chloride

Total 100.0


Process: 

1. Add Phase 2 ingredients and mix with a homogenizer and heat part 2 and 3 to 75-80oC.

2. When all the Carnauba wax and microcrystalline wax are melt, slurry in Phase 1 and stir until homogenous. 

3. Add Phase 3 heated to 75-80oC into Phase 2 heated to 75-80oC and stir until homogenous. Fill into appropriate container.
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 

Page 1 of 2
This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 

                                                                                                                                                                        Page 2 of 2                                                                                                                                                                        


_1303134405.xls
Sheet1

		Ingredients		% (w/w)		Functions		INCI Designation		Supplier

		Phase 1

		ASO-I2		5.0		Powdery thickening agent		Aluminium Starch Octenylsuccinate (and) Isopropyl Titanium Triisostearate		Kobo

		Sericite J		3.0		Filler		Mica		Kobo

		MSS-500/3H		5.0		Silicone slip agent and absorbent		Silica		Kobo

		SP-500		4.0		Provides creamy feel and absorbent		Nylon-12		Kobo

		SPCAT-I2		4.0		Improves skin feel and provides powdery after feel		Talc (and) Ethylene/Methacrylate copolymer (and) Isopropyl Titanium Triisostearate		Kobo

		Phase 2

		WE70U		10.0		Pigmentary grade dispersion (White)		Titanium Dioxide (and) Polyglyceryl-4 Isostearate (and) Cetyl Dimethicone Copolyol (and) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE55Y		1.4		Pigmentary grade dispersion (Yellow)		Iron Oxide (CI 77492) (and) Polyglyceryl-4 Isostearate (and) Cetyl Dimethicone Copolyol (and) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE70R		0.5		Pigmentary grade dispersion (Red)		Iron Oxide (CI 77491) (and) Polyglyceryl-4 Isostearate (and) Cetyl Dimethicone Copolyol (and) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		WE70B		0.1		Pigmentary grade dispersion (Black)		Iron Oxide (CI 77499) (and) Polyglyceryl-4 Isostearate (and) Cetyl Dimethicone Copolyol (and) Hexyl Laurate (and) Isopropyl Titanium Triisostearate		Kobo

		TNP50VTTS		20.0		UV Filter		C12-15 Alkyl Benzoate (and) Titanium Dioxide (and) Alumina (and) Polyhydroxystearate (and) Isopropyl Titanium Triisostearate (and) Triehoxy Caprylsilane		Kobo

		BC20cs		6.0		Slip agent		Dimethicone		Basildon

		Cocoate BG		10.0		Emollient		Butylene Glycol Cocoate		Gattefosse

		Plurol Diisostearique		6.0		w/o, PEG-free emulsifier		Polyglyceryl-3 Diisostearate		Gattefosse

		Compritol 888 ATO		0.5		Thickener for oils		Glyceryl Dibehenate (and) Tribehenin (and) Glyceryl Behenate		Gattefosse

		Carnauba Wax		4.0		Thickener		Copernicia Cerifera (Carnauba) Wax

		Lipocire A		3.0		Emollients and improves skin feel		Hydrogenated Palm Kernel Glycerides (and) Hydrogenated Palm Glycerides		Gattefosse

		Preservatives		0.3		Preservatives

		Phase 3

		Water		15.4

		Salt		1.8		Stabilizer		Sodium Chloride

		Total		100.0
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		Ingredients		% (w/w)		Functions		INCI Designation		Supplier

		TNP50VTTS		20.0		UV Filter		C12-15 Alkyl Benzoate (and) Titanium Dioxide (and) Alumina (and) Polyhydroxystearate (and) Isopropyl Titanium Triisostearate (and) Triehoxy Caprylsilane		Kobo

		BC20cs		6.0		Slip agent		Dimethicone		Basildon

		Cocoate BG		10.0		Emollient		Butylene Glycol Cocoate		Gattefosse

		Plurol Diisostearique		6.0		w/o, PEG-free emulsifier		Polyglyceryl-3 Diisostearate		Gattefosse

		Compritol 888 ATO		0.5		Thickener for oils		Glyceryl Dibehenate (and) Tribehenin (and) Glyceryl Behenate		Gattefosse

		Carnauba Wax		4.0		Thickener		Copernicia Cerifera (Carnauba) Wax

		Lipocire A		3.0		Emollients and improves skin feel		Hydrogenated Palm Kernel Glycerides (and) Hydrogenated Palm Glycerides		Gattefosse

		Preservatives		0.3		Preservatives

		Phase 3

		Water		15.4

		Salt		1.8		Stabilizer		Sodium Chloride

		Total		100.0






