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Phase 1

Emullium Delta 6 O/W Emulsifier Cetyl alcohol (and) glyceryl 

stearate (and) PEG-75 Stearate 

(and) Ceteth-20 (and) Steareth-20

Gattefosse

Lipocire A 4 Texture Agent Hydrogenated Palm Kernel 

Glycerides (and) Hydrogenated 

Palm Glycerides

Gattefosse

Labrafac CC 2 Emollient Capric/Caprylic Triglycerides Gattefosse

BC Volatile 5 6 Feeling Agent Cyclomethicone Basildon

Isostearyl Isostearate 4 Emollient Isostearyl Isostearate Gattefosse

Floramac 10 3 Emollient Ethyl Macadamiate (and) 

Tocopherol (and) Malic Acid

Floratech

Phase 2

DI Water 67 Water Water

Ultrez 20 0.3 Gelling Agent Ultrez 20

Xanthan Gum 0.2 Gelling Agent Xanthan Gum

Phase 3

Sodium Hydroxide 0.6 Neutralizing Agent Sodium Hydroxide

Phase 4

ASO-I2 3 Powder Aluminum Starch 

Octenylsuccinate (And) Isopropyl 

Titanium Triisostearate

KOBO

Phase 5

Preservative 0.8 Preservative Preservative

Gatuline In-Tense 2 Anti-aging Active Capric/Caprylic Triglycerides (and) 

Spilanthes Acmella Flower Extract

Gattefosse

Fragrance 0.3 Perfume Perfume


[image: image4.png]






CA1070 Cocoon Cream
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Phase 6

FDC Yellow 0.75 Yellow Dye Yellow Dye

Blue Dye 0.05 Blue Dye Blue Dye

Total 100


Process: 

1. Under stirring, disperse Ultrez 20 into water of phase 2 at room temperature and let it to stand.  Add in xanthan gum and stir and continue stirring and heat to 80°C.

2. Mix the ingredients of phase 1 and heated to 80°C.

3. Under rapid stirring, add 2 to 1 and stir for about 5 mins.

4. Add phase 3 and maintain rapid stirring for about 3mins.

5. Cool under moderate planetary stirring and at about 35°C, add the others ingredients.

6. Complete cooling
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 
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		Ingredients		% (w/w)		Functions		INCI designation		Supplier

		Phase 1

		Emullium Delta		6		O/W Emulsifier		Cetyl alcohol (and) glyceryl stearate (and) PEG-75 Stearate (and) Ceteth-20 (and) Steareth-20		Gattefosse

		Lipocire A		4		Texture Agent		Hydrogenated Palm Kernel Glycerides (and) Hydrogenated Palm Glycerides		Gattefosse

		Labrafac CC		2		Emollient		Capric/Caprylic Triglycerides		Gattefosse

		BC Volatile 5		6		Feeling Agent		Cyclomethicone		Basildon

		Isostearyl Isostearate		4		Emollient		Isostearyl Isostearate		Gattefosse

		Floramac 10		3		Emollient		Ethyl Macadamiate (and) Tocopherol (and) Malic Acid		Floratech

		Phase 2

		DI Water		67		Water		Water

		Ultrez 20		0.3		Gelling Agent		Ultrez 20

		Xanthan Gum		0.2		Gelling Agent		Xanthan Gum

		Phase 3

		Sodium Hydroxide		0.6		Neutralizing Agent		Sodium Hydroxide

		Phase 4

		ASO-I2		3		Powder		Aluminum Starch Octenylsuccinate (And) Isopropyl Titanium Triisostearate		KOBO

		Phase 5

		Preservative		0.8		Preservative		Preservative

		Gatuline In-Tense		2		Anti-aging Active		Capric/Caprylic Triglycerides (and) Spilanthes Acmella Flower Extract		Gattefosse

		Fragrance		0.3		Perfume		Perfume

		Phase 6

		FDC Yellow		0.75		Yellow Dye		Yellow Dye

		Blue Dye		0.05		Blue Dye		Blue Dye

		Total		100
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		Ingredients		% (w/w)		Functions		INCI designation		Supplier

		Phase 6

		FDC Yellow		0.75		Yellow Dye		Yellow Dye

		Blue Dye		0.05		Blue Dye		Blue Dye

		Total		100






