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Phase 1

Emulium Kappa 6 O/W Emulsifier Candelila/Jojoba/Rice Bran 

Polyglyceryl-3 Esters (and) 

Glyceryl Stearate (and) Cetearyl 

Alcohol (and) Sodium Stearoyl 

Lactylate

Gattefosse

Cetyl Alcohol 2 Thickener Cetyl Alcohol

Labrafac CC 4 Emollient Caprylic/Capric Triglyceride Gattefosse

MOD 4 Emollient Octyldodecyl Myristate Gattefosse

Geleol Pastilles 2 Thickener Glyceryl Stearate Gattefosse

Florasun 90 2 Emollient Sunflower Oil Floratech

Phase 2

Deionised Water 74

Lucentite SWN 0.5 Rheology modifier Lithium Magensium Sodium  Kobo

Phase 3

Glycerine 5 Humectant

Xanthan Gum 0.3 Gelling agent Xanthan Gum

Phase 4

Microcare MTP 0.2 Preservatives

Total 100
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CA 1097 Rich Cream
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Process: 

1. Add Lucentite SWN into deioinised water and mix well.

2. Premix Xanthan Gum with Glycerine and stir until homogenous.

3. Add Phase 3 into Phase 1 and stir until homogenous.

4. Add Phase 2 heated to 75oC into Phase 2+3 heated to 75oC with moderate stirring.

5. Homogenize the mixture for about 5 minutes.

6. Cool while stirring with moderate planetary agitation.

7. Add in Phase 4 into Phase 1+2+3 at 45oC.

8. Complete cooling.
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This formula is presented in good faith, and we believe it is correct, but no warranty as to accuracy of results, or fitness for a particular use is given, nor is freedom from patent infringement to be inferred. It’s offered solely for your consideration, investigation and verification. 
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		Ingredients		%(w/w)		Functions		INCI designation		Supplier

		Phase 1

		Emulium Kappa		6		O/W Emulsifier		Candelila/Jojoba/Rice Bran Polyglyceryl-3 Esters (and) Glyceryl Stearate (and) Cetearyl Alcohol (and) Sodium Stearoyl Lactylate		Gattefosse

		Cetyl Alcohol		2		Thickener		Cetyl Alcohol

		Labrafac CC		4		Emollient		Caprylic/Capric Triglyceride		Gattefosse

		MOD		4		Emollient		Octyldodecyl Myristate		Gattefosse

		Geleol Pastilles		2		Thickener		Glyceryl Stearate		Gattefosse

		Florasun 90		2		Emollient		Sunflower Oil		Floratech

		Phase 2

		Deionised Water		74

		Lucentite SWN		0.5		Rheology modifier		Lithium Magensium Sodium Silicate		Kobo

		Phase 3

		Glycerine		5		Humectant

		Xanthan Gum		0.3		Gelling agent		Xanthan Gum

		Phase 4

		Microcare MTP		0.2		Preservatives

		Total		100






